## Slide 1: Effect of Alloying Element in Iron- Carbide Phase Diagram
Powerpoint Templates
Powerpoint Templates Page 1

## Slide 2: Effects of alloying elements
Powerpoint Templates
Page 2
Alloying elements have significant effect on the iron-iron carbide equilibrium diagram
The effect of the alloying element in the steel may be one or more of the following:
It may go into solid solution in the iron,
enhancing the strength.
Hard carbides associated with Fe,C may be formed.
It may form intermediate compounds with iron, e.g. FeCr (sigma phase), FeW.
It may influence the critical range in one or
more of the following ways:

## Slide 3: Effects of alloying elements
Powerpoint Templates
Page 3
Alter the temperature. For e.g, 3% Ni lowers the Ac points some 30°C, while 12% Cr raises the Ac1, temperature to about 800°C
Alter the carbon content of the eutectoid: The C content of the pearlite in a 12% Cr steel is 0.33%, as compared with 0.87 in an ordinary steel. Ni also reduces the amount of C in the pearlite and consequently increases the volume of this constituent at the expense of the weaker ferrite.
Alter the “critical cooling velocity”, which is the minimum cooling speed which will produce bainite or martensite from austenite.

## Slide 4: Effects of alloying elements
Powerpoint Templates
Page 4
 Some alloying elements will widen the temperature range through which austenite is stable while other elements will constrict the temperature range.
 Combinations of elements can be chosen so that the volume change is reduced and also the risk of quench cracking.
 It may have a chemical effect on the impurities. Under suitable slag conditions vanadium, in quite small quantities, "cleans" the steel and renders it free from slag inclusions. Manganese and zirconium form sulphides.
 Some elements (like Al, Cr, Si, Cu) tends to produce adherent oxide film on steel which resist
corrosion and oxidation at elevated temps.

## Slide 5: Effects of alloying elements
Powerpoint Templates
Page 5
 Creep strength may be increased by the presence of a dispersion of fine carbides, e.g. molybdenum.
 It may render the alloy sluggish to thermal changes, increasing the stability of the hardened condition and so producing tool steels which are capable of being used up to 550°C without softening and in certain cases may exhibit an increase in hardness.

## Slide 6: Why we do alloying in steel?
Powerpoint Templates
Page 6

## Slide 7: Effect of alloying elements
Powerpoint Templates
Page 7
Fig. – Effect of alloying elements on hardness of steel
Fig. – Effect of alloying elements on eutectoid temp. and
C content

## Slide 8: Effect of alloying elements
Powerpoint Templates

## Slide 9: Effect of alloying elements
Powerpoint Templates
Fig. – Effect of different % of C in the presence of Cr in steel

## Slide 10: Effect of alloying elements
Powerpoint Templates
Table I – Effect of alloying on critical cooling speed on steel
Carbon, % | Alloying Element, % | Cooling Speed to form Martensite, °C per sec (650°C)
0.42 | 0.55 Mn | 550
0.40 | 1.60 Mn | 50
0.42 | 1.12 Ni | 450
0.40 | 4.80 Ni | 85
0.38 | 2.64 Cr | 10

## Slide 11: General Trends of alloying
Powerpoint Templates

## Slide 12: General Trends of alloying
Powerpoint Templates
Page 12

## Slide 13: Classification of alloying elements
Powerpoint Templates
Elements which tend to form carbides. Cr, W, Ti, Cb, V, Mo, Zr and Mn. Generally carbide formers are also ferrite formers. M23C6, M6C, etc. The mixture of complex carbides is often referred to as cementite.
Elements which tend to graphitise the carbide. Si, Co, Al and Ni. Only a small proportion of these elements can be added to the steel before graphite forms during processing, with attendant ruin of the properties of the steel. Their presents makes the carbides unstable.
Elements which tend to form nitrides. All carbide forming elements are also nitride former.

## Slide 14: Classification of alloying elements
Powerpoint Templates
Elements which tend to stabilise austenite. Mn, Ni, Co and Cu. These elements alter the critical points of iron in a similar way to carbon by raising the A4 point and lowering the A3 point, thus increasing the range in which austenite is stable, and they also tend to retard the separation of carbides.
Elements which tend to stabilise ferrite. Cr, W, Mo, V and Si.

## Slide 15: Austenite/Ferrite Stabilizers
Powerpoint Templates
 Different elements have solubilities in alpha and gamma iron
 Binary phase diagram is used to explain

## Slide 16: Austenite/Ferrite Stabilizers
Powerpoint Templates
Figs. – Two types of phase equilibrium diagrams for Fe

## Slide 17: Ferrite Stabilizers
Powerpoint Templates
Al, Cr, Si, Mo, W, P, are ferrite stabilizers, they tend to form solid solution with alpha iron
 They have greater solubility in ferrite – BCC
 Generally have similar BCC structure
 They decrease the amount of C present in γ-Fe
 Favors formation of free carbides in steel
 The ferrite form is Delta ferrite since it can exists from melting point to room temp.

## Slide 18: Ferrite Stabilizers
Powerpoint Templates

## Slide 19: Ferrite Stabilizers
Powerpoint Templates
Fig. - Effect of C on Fe-Cr diagram

## Slide 20: Ferrite Stabilizers
Powerpoint Templates
Page 20
Fig. – Effect of Cr on critical temp. and γ phase transformation in steel

## Slide 21: Austenite Stabilizers
Powerpoint Templates
Ni, Mn, Co are austenite stabilizers, they tend to form solid solution with gamma iron
 They have greater solubility in austenite
 They have FCC crystal structure
 They do not combine with C present in γ to form simple or complex carbide, therefore C remains in the solid solution in the γ
 13% Mn steels are austenitic at room temp. called Hadfield Steel.
 C and N are also austenite stablizers (interstitial solutes in fcc)

## Slide 22: Austenite Stabilizers
Powerpoint Templates

## Slide 23: Austenite Stabilizers
Powerpoint Templates
Page 23
Fig. – Effect of Mn on critical temp. and γ phase transformation in steel

## Slide 24: Schaeffler diagram
Powerpoint Templates
Page 24
 Schaeffler and Delong diagrams are used to predict structure on the basis of alloying elements
 Plots the compositional limits at room temperature of austenite, ferrite and martensite, in terms of nickel and chromium equivalents
 The Cr and Ni equivalent can be empirically determined as:
Cr equivalent = (Cr) + 2(Si) + 1.5(Mo) + 5(V) + 5.5(Al) + 1.75(Nb) + 1.5(Ti) + 0.75(W)
Ni equivalent = (Ni) + (Co) + 0.5(Mn) + 0.3(Cu) +
25(N) + 30(C)

## Slide 25: Schaeffler diagram
Powerpoint Templates

## Slide 26: Modified Schaeffler diagram
Powerpoint Templates
 Delong modified the schaeffler diagram
 Ferrite no. is also plotted on schaeffler diagram
 Effect of nitrogen was also taken into account
Widely use in predicting phase-structure in weld metal
 Also include calculation of volume and composition of carbide phase

## Slide 27
Powerpoint Templates
Modified Schaeffler diagram
Page 27

## Slide 28: Schaeffler-Delong diagram
Powerpoint Templates
FN = Ferrite No.
Low %ferrite leads to solidification cracking in weld metal, but low
%ferrite render SS more corrosion resistant

## Slide 29: Schaeffler-Delong diagram
Powerpoint Templates

## Slide 30: Modified Schaeffler diagram
Powerpoint Templates
 FN can be roughly determine by: FN = 3.34 Creq – 2.46 Nieq – 28.6
--> FN between 3-7 (max.) is preferred
Solidification mode of S.S. during casting or welding can be predicted roughly as under:
 Creq/Nieq < 1.5
 Creq/Nieq > 2.0
(Austenitic) (Ferritic)
 In b/w 1.5 and 2.0 is the mixed structure